SUBMISSION ROLE: 2015 Northwest Regional Meeting. ABSTRACT SYMPOSIUM NAME: Interfaces and Electrochemistry for Energy Applications and Beyond - Oral - Invited. CONTROL ID: 2220656. TITLE: Enhanced Efficiency of Organic and Perovskite Photovoltaics from Shape-Dependent Broadband Plasmonic Effects of Silver Nanoplates. PRESENTER: Chih-Ping Chen. PRESENTER (E-MAIL ONLY): cpchen@mail.mcut.edu.tw. AUTHORS (FIRST NAME, LAST NAME): Chih-Ping Chen1. INSTITUTIONS (ALL): 1. Materials Engineering, Ming Chi University of Technology, New Taipei City, Taiwan.. PRESENTATION TYPE: Oral Preferred. ABSTRACT BODY: Abstract: In this study, we systematically investigated the plasmonic effects of silver nanoplates (Ag NPs) embedded in organic and perovskite (PVSK) photovoltaic (PV) cells. Optical properties of the Ag NPs were manipulated by varying their sizes and shapes through controllable wet chemical processes. As the lengths of the edges of the Ag NPs increased, their surface plasmon resonance bands broadened, with the maximum extinction wavelength extending to as far as 750 nm. After embedding various types of Ag NPs into the PEDOT:PSS [poly(3,4-ethylenedioxythiophene)/polystyrenesulfonate] layer, the short-circuit photocurrent density increased by 7.6–17.5%, relative to that of the pre-optimized control PVs, with the power conversion efficiency(PCE) increasing by up to 13%. We obtained an optimized PCE of 8.5% for normal PVSK device under simulated AM 1.5G irradiation (100 mW cm–2). After the incorporation of Ag NPs, a much higher PCE of 9.6% was obtained. External quantum efficiencies were increased significantly as a result of the increased plasmonic scattering effect of Ag NPs.. DECISION STATUS:. ABSTRACT STATUS: resubmitted Withdraw.

SUBMISSION ROLE: 2015 Northwest Regional Meeting. ABSTRACT SYMPOSIUM NAME: Interfaces and Electrochemistry for Energy Applications and Beyond - Oral - Invited. CONTROL ID: 2221235. TITLE: Electrolyte Performance for Na-ion Batteries. PRESENTER: Riley Parrish. PRESENTER (E-MAIL ONLY): rileyparrish@boisestate.edu. AUTHORS (FIRST NAME, LAST NAME): Riley Parrish2, Hui Xiong2, Eric J. Dufek1. INSTITUTIONS (ALL): 1. Energy Storage and Transportation Systems, Idaho National Laboratory, Idaho Falls, ID, United States. 2. MSE/2090, Boise State University, Boise, ID, United States.. PRESENTATION TYPE: Oral Preferred. ABSTRACT BODY: Abstract: Sodium ion (Na-ion) batteries have been viewed as a low cost alternative to lithium ion (Li-ion) technology for large scale applications such as grid energy storage. Na-ion batteries are still a relatively young and developing technology and, therefore, many of the components do not meet the quality or performance standards of current Li-ion batteries. The solid-electrolyte interphase (SEI), a thin passivation layer formed on the anode during early cycling, is crucial to the performance and lifetime of the electrode. However, impurities present in the electrolyte during formation can have a significant effect on the structure and stability of the SEI over the lifetime of the battery, reducing efficiency and causing dramatic capacity loss. In order to optimize the long term performance of the electrode, the formation dynamics and effects of electrolyte impurities on SEI formation need to be better understood. In this work, we look to characterize the effects of electrolyte impurities on SEI formation on inert, surrogate electrodes. Electrolyte properties, such as ionic conductivity, viscosity, and water content, were measured for electrolytes prepared using as-received components, and subsequently repeated after a purification and filtration process. Cyclic voltammetry (CV) was then used to characterize the electrochemical performance of the electrolytes, while spectroscopic ellipsometry (SE) was performed in parallel to observe SEI growth and stability as a result of the electrolyte characteristics.. DECISION STATUS:. ABSTRACT STATUS: submitted Withdraw.

SUBMISSION ROLE: 2015 Northwest Regional Meeting. ABSTRACT SYMPOSIUM NAME: Interfaces and Electrochemistry for Energy Applications and Beyond - Oral - Invited. CONTROL ID: 2247736. TITLE: Organic electrode materials and their applications in rechargeable batteries. PRESENTER: Burak Esat. PRESENTER (E-MAIL ONLY): besat@fatih.edu.tr. AUTHORS (FIRST NAME, LAST NAME): Burak Esat1, Sumeyye Bahceci-Sertkol1, Anton Momchilov2. INSTITUTIONS (ALL): 1. Chemistry, Fatih University, Istanbul, Turkey. 2. Institute of Electrochemistry and Energy Systems, Bulgarian Academy Of Sciences, Sofia, Bulgaria.. PRESENTATION TYPE: Oral Only. ABSTRACT BODY: Abstract: The ever-increasing demand for high-performing, light weight, economical, and safe power storage for high–tech portable devices and electric vehicles leads to augmented research efforts in the field of organic or organic/hybrid materials to be used as electrodes in energy storage devices. There has recently been an increasing number of studies toward the development of novel pure or composite materials containing redox polymers with pendant organic electro-active groups which may be used as cathode- or anode-active material in batteries. These efforts may eventually lead to totally organic batteries with improved properties such as light weight, flexibility, improved environmental safety, low cost of manufacturing. We hereby represent novel polymers and reduced graphene oxide materials with pendant electro-active groups such as TEMPO, benzimidazole-1-oxyl-3-oxides and quinones. The first example of polymers with pendant anode-active groups studied in our group is a polymethacrylate derivative carrying anthraquinone moieties (pMAntrq). A battery which utilizes a composite material made of this compound mixed with carbon conductivity agent against lithium metal (AQ¦1M LiClO4 in EC:DEC=1:1¦ Li) had an initial discharge capacity of 151 mAh/g . This material was also used in an aqueous battery (AQ¦5M KOH aq.¦LiMn2O4) and had an initial discharge capacity of 37.7 mAh/g. This is the first reported example of such organic-inorganic hybrid battery. An anode material based on reduced graphene oxide (rGO) functionalized with anthraquinone is also investigated. The initial studies against Li metal revealed that a quite reversible capacity of 200 mAh/g was obtained based on the weight of electro-active anthraquinone moieties when cycled between 3.2 and 1.8 V at 0.3C rate.. DECISION STATUS:. ABSTRACT STATUS: resubmitted Withdraw.

SUBMISSION ROLE: 2015 Northwest Regional Meeting. ABSTRACT SYMPOSIUM NAME: Interfaces and Electrochemistry for Energy Applications and Beyond - Oral - Invited. CONTROL ID: 2281186. TITLE: Electrochemical energy storage characteristics of CaB6. PRESENTER: Krishnan Raja. PRESENTER (E-MAIL ONLY): ksraja@uidaho.edu. AUTHORS (FIRST NAME, LAST NAME): Kalyan Chitrada1, Raghunath Kanakala2, Krishnan Raja1. INSTITUTIONS (ALL): 1. Chemical and Materials Engineering, University of Idaho, Moscow, ID, United States. 2. Industrial Technology, University of Idaho, Idaho Falls, ID, United States.. PRESENTATION TYPE: Oral Only. ABSTRACT BODY: Abstract: Calcium hexaboride has a body centered cubic lattice structure that belongs to the space group of Pm3m-O1h. The B6-octahedra are located at the corners of the cubic lattice. The divalent cations are inserted into the network of boron cages and located at the center of the cube. This type of lattice structure forms a tunnel like morphology that enables the cations to be easily removed and inserted. CaB6 can easily form Ca vacancies and become cation deficient. Presence of these point defects makes the material a semiconductor and also increases the sites for intercalation of ions leading to charge storage. Commercially available CaB6 material was investigated as the electrode material for electrochemical super capacitors in 1 M LiPF6 organic electrolytes. Galvanostatic charge-discharge experiments were carried out at different current densities in the range of 0.1 – 1 A/g using a three-electrode configuration with a silver wire as a quasi-reference electrode. A diffusion controlled pseudo-capacitance behavior was observed in the lithiated electrolyte. Analysis of the Warburg impedance behavior revealed a diffusion coefficient in the range of 10-8 -10-9 cm2/s. Mott-Schottky plots of the CaB6 in LiPF6 electrolyte revealed a distinct p-type semiconductivity indicating presence of Ca vacancies in the order of 1021 cm-3. The capacitance of the commercial micro-crystalline CaB6 was not significant (~20 - 40 F/g). However, CaB6 could be a potential energy storage material when prepared in the form of defect modulated nanostructure.. DECISION STATUS:. ABSTRACT STATUS: submitted Withdraw.

SUBMISSION ROLE: 2015 Northwest Regional Meeting. ABSTRACT SYMPOSIUM NAME: Interfaces and Electrochemistry for Energy Applications and Beyond - Oral - Invited. CONTROL ID: 2282172. TITLE: Ordered Arrays of Nanotubular/Nanoporous Oxides of Transition Metals for Electrochemical Energy Storage. PRESENTER: Krishnan Raja. PRESENTER (E-MAIL ONLY): ksraja@uidaho.edu. AUTHORS (FIRST NAME, LAST NAME): Krishnan Raja1. INSTITUTIONS (ALL): 1. Chemical and Materials Engineering, University of Idaho, Moscow, ID, United States.. PRESENTATION TYPE: Oral Only. ABSTRACT BODY: Abstract: Vertically oriented and well-ordered nanotubular arrays or nanoporous oxide layer could be obtained by a simple process of electrochemical anodization of transition metals such as Fe, Ti, Zr, and W and their alloys. The choice of formation of either nanotubular or nanoporous oxide structure was observed to be a strong function of oxygen solubility in the metal structure, and the electrochemical parameters that balanced the surface perturbation. The anodic transition metal oxide layers inherently contained high concentration of oxygen vacancies that could be modulated during the post-anodization thermal annealing process under controlled atmospheres by purging with reducing, inert, or reducing gases. The point defect density of the anodic oxides played a significant role determining the electrochemical energy storage characteristics. Nanotubular arrays of oxide layers were synthesized by anodizing Ti, W, and Zr-W alloy. The electrochemical energy storage characteristics of these oxide samples were evaluated in 0.5 M H2SO4, 1 M LiCl, and 1 M NaOH electrolytes using cyclic voltammetry, electrochemical impedance spectrometry, and galvanostatic charge-discharge techniques. The nanostructured oxide layers showed an areal capacitance of > 60 mF/cm2 and a specific capacitance of > 300 F/g.. DECISION STATUS:. ABSTRACT STATUS: submitted Withdraw.

SUBMISSION ROLE: 2015 Northwest Regional Meeting. ABSTRACT SYMPOSIUM NAME: Interfaces and Electrochemistry for Energy Applications and Beyond - Oral - Invited. CONTROL ID: 2282718. TITLE: Electrochemical Atomic Layer Deposition (E-ALD). PRESENTER: John Stickney. PRESENTER (E-MAIL ONLY): stickney@uga.edu. AUTHORS (FIRST NAME, LAST NAME): John L. Stickney1. INSTITUTIONS (ALL): 1. Univ of Georgia, Athens, GA, United States.. PRESENTATION TYPE: Oral Only. ABSTRACT BODY: Abstract: The talk will concern the electrochemical form of ALD (E-ALD). ALD is the deposition of materials an atomic layer at a time via surface limited reactions using a cycle. Electrochemical surface limited reactions are referred to as underpotential deposits (UPD). UPD is the use of a potential prior to (under) that needed to deposit the bulk element. UPD results from the free energy of formation of a surface compound or alloy. A wide range of materials have been formed (see figure), including most of the II-VI compounds such as CdTe and MCT, and some of the III-V compounds, including GaSb and InSb. Photovoltaic materials such as CIS (CuInSe2) and CIGS (CuInGaSe2) have been formed as well. Different nano structures have been grown including: Superlattices, nanoclusters and more recently nanowires. Metal films such as Pt, Pd, and Ru have also been grown for energy storage and fuel cell catalysis, along with alloys such as PtRu. Materials of importance in the electronics industry for the formation of ULSI have been formed for barrier and seed layers, including Cu and Ru. Phase change materials, such as GeSbTe (GST), have been formed with a wide range of stoichiometries, and a cycle for the formation of Ge has also been developed. This talk will describe the principles and concepts of E-ALD, as well as hardware and cycle chemistries. In general, crystalline deposits are formed from aqueous solutions at room temperature, without annealing, on conducting and semiconducting surfaces. Deposits show linear growth with cycle #, at growth rates generally between 0.1 and 0.2 nm/cycle for metals, and 0.2 to 0.4 nm/cycle for compounds. Cycle times are generally 60 s/cycle or less. Atomically flat deposits have been observed with STM on polycrystalline substrates, suggesting surface smoothing may be occurring. This appears to result from the deposits forming under equilibrium conditions: under potential control. II-VI: CdS, CdSe, CdTe, ZnS, ZnSe, ZnTe, HgSe, HgTe, HgS, HgCdTe III-V: GaSb, InAs, InSb IV-VI: PbS, PbSe, PbTe Other: In2Se3, CuSe, Sb2Te3, Bi2Te3, CuInSe2, Cu(InGa)Se2, CuGaSe2, GexSbyTez, Superlattices: InAs/InSb, PbSe/PbTe Nanoclusters: In2Se3, PbSe, HgSe, CdTe Elemental: Pt, Cu, Ag, Pd, Ru, Au, Ge Alloys: PtRu Substrates: Au, Ag, Cu, InP, Pt, ITO, FTO, GaAs, Ru. DECISION STATUS:. ABSTRACT STATUS: submitted Withdraw.

SUBMISSION ROLE: 2015 Northwest Regional Meeting. ABSTRACT SYMPOSIUM NAME: Interfaces and Electrochemistry for Energy Applications and Beyond - Oral - Invited. CONTROL ID: 2283715. TITLE: Metabolon Bioelectrocatalysis for Biofuel Cells. PRESENTER: Shelley Minteer. PRESENTER (E-MAIL ONLY): minteer@chem.utah.edu. AUTHORS (FIRST NAME, LAST NAME): Shelley D. Minteer1. INSTITUTIONS (ALL): 1. University of Utah, Salt Lake City, UT, United States.. PRESENTATION TYPE: Oral Only. ABSTRACT BODY: Abstract: Metabolons are supercomplexes of sequential metabolic pathway enzymes that channel substrate from one enzyme in the pathway to the next. They are critical for the high flux through metabolic pathways, including the Krebs cycle and the electron transport chain. This presentation will discuss the use of in-vivo and in-vitro metabolons for enzymatic bioelectrocatalysis. We will discuss biofuel cells for chemical energy conversion to electricity utilizing these natural and synthetic metabolons.. DECISION STATUS:. ABSTRACT STATUS: submitted Withdraw.

SUBMISSION ROLE: 2015 Northwest Regional Meeting. ABSTRACT SYMPOSIUM NAME: Interfaces and Electrochemistry for Energy Applications and Beyond - Oral - Invited. CONTROL ID: 2285446. TITLE: Earth-Abundant Electrocatalysts of Overall Water Splitting. PRESENTER: Yujie Sun. PRESENTER (E-MAIL ONLY): yujie.sun@usu.edu. AUTHORS (FIRST NAME, LAST NAME): Yujie Sun1. INSTITUTIONS (ALL): 1. Chemistry and Biochemistry, Utah State University, Logan, UT, United States.. PRESENTATION TYPE: Oral Only. ABSTRACT BODY: Abstract: Water splitting with renewable energy input to produce hydrogen and oxygen has been widely considered as an attractive approach to convert and store renewable energy sources in chemical forms. Owing to the sluggish kinetics of its both half reactions, overall water splitting necessitates the development of competent catalysts. Solid-state catalysts employing noble metals, such as platinum and iridium, have long been recognized as effective catalysts for hydrogen and oxygen evolution reactions, respectively, however the associated scarce and high cost limit their application on a large scale. It remains a great challenge to develop earth-abundant water splitting catalysts exhibiting both high efficiency and strong robustness in aqueous media. Our group focus on exploring 1st-row transition metal catalysts for electrocatalytic water splitting in aqueous media. Facile electrochemical and microwave-assisted synthetic approaches were employed to produce various nano-structured catalysts with low energy cost. A suite of surface characterization and electrochemical techniques were applied to study the composition-structure-activity relationships of these catalysts. Coupled with theoretical computation, our work will provide guidance for the rational design and development of improved and low-cost catalysts of overall water splitting, paving the way towards artificial photosynthesis.. DECISION STATUS:. ABSTRACT STATUS: submitted Withdraw.

SUBMISSION ROLE: 2015 Northwest Regional Meeting. ABSTRACT SYMPOSIUM NAME: Interfaces and Electrochemistry for Energy Applications and Beyond - Oral - Invited. CONTROL ID: 2290182. TITLE: Physical Models for Charge Transfer at Single Crystal Oxide Semiconductor Surfaces as Revealed by the Doping Density Dependence of Collection Efficiency of Dye Sensitized Photocurrents. PRESENTER: Bruce Parkinson. PRESENTER (E-MAIL ONLY): bparkin1@uwyo.edu. AUTHORS (FIRST NAME, LAST NAME): Bruce A. Parkinson1. INSTITUTIONS (ALL): 1. Chemistry, University of Wyoming, Laramie, WY, United States.. PRESENTATION TYPE: Oral Only. ABSTRACT BODY: Abstract: The doping density dependence of photocurrents has been experimentally measured at single crystal rutile TiO2 electrodes sensitized with the N3 chromophore and a trimethine dye. As the doping density of the electrodes was varied from 1015 cm-3 to 1020 cm-3, three different regimes of behavior were observed for the magnitude and shape of the dye sensitized current-voltage curves. Low-doped crystals produced current-voltage curves with a slow rise of photocurrent with potential. At intermediate doping levels, Schottky barrier behavior was observed producing a photocurrent plateau at electrode bias in the depletion region. At highly doped electrodes tunneling currents played a significant role especially in the recombination processes. These different forms of the current-voltage curves could be fit to an Onsager-based model for charge collection at a semiconductor electrode. The fitting revealed the role of the various physical parameters that govern photoinduced charge collection in sensitized systems.. DECISION STATUS:. ABSTRACT STATUS: submitted Withdraw.

SUBMISSION ROLE: 2015 Northwest Regional Meeting. ABSTRACT SYMPOSIUM NAME: Interfaces and Electrochemistry for Energy Applications and Beyond - Oral - Invited. CONTROL ID: 2292537. TITLE: The Complete Oxidation of Glycerol to CO2: A Hybrid Enzymatic and Organic Electrocatalytic Cascade. PRESENTER: David Hickey. PRESENTER (E-MAIL ONLY): dhickeychem@gmail.com. AUTHORS (FIRST NAME, LAST NAME): David Hickey3, Matthew S. McCammant3, Matthew S. Sigman1, Shelley D. Minteer2. INSTITUTIONS (ALL): 1. Univ of Utah, Salt Lake City, UT, United States. 2. University of Utah, Salt Lake City, UT, United States. 3. Chemistry, University of Utah, Salt Lake City, UT, United States.. PRESENTATION TYPE: Oral Only. ABSTRACT BODY: Abstract: There has been a significant interest lately in the complete oxidation of biofuels to CO2. The use of multiple biocatalysts allows for deeper biofuel oxidation and thus maximizes the energy density that can be extracted per molecule of biofuel. However, there are still many biofuels for which a suitable biocatalyst is not known. We have recently taken an alternative approach to combine the high catalytic activity of enzymatic biocatalysts with the promiscuous nature of small molecule organic catalysts. We demonstrate the complete electrochemical oxidation of the biofuel glycerol to CO2 using a hybrid enzymatic and small-molecule catalytic system. Combining an enzyme, oxalate oxidase, and an organic oxidation catalyst, 4-amino-TEMPO, we are able to electrochemically oxidize glycerol at a carbon electrode, while collecting as many as 16 e-s per molecule of fuel. We also investigate the anomalous electrocatalytic properties that allow 4-amino-TEMPO to be active under the acidic conditions required for oxalate oxidase to function, and demonstrate how these properties can be utilized to design highly active bioanode materials.. DECISION STATUS:. ABSTRACT STATUS: submitted Withdraw.

SUBMISSION ROLE: 2015 Northwest Regional Meeting. ABSTRACT SYMPOSIUM NAME: Interfaces and Electrochemistry for Energy Applications and Beyond - Oral - Invited. CONTROL ID: 2299129. TITLE: New method for solid electrolyte interphase characterization and fast electrolyte selection for alkali(-ion) batteries. PRESENTER: Sergiy Sazhin. PRESENTER (E-MAIL ONLY): sergiy.sazhin@inl.gov. AUTHORS (FIRST NAME, LAST NAME): Sergiy Sazhin1, Kevin Gering1, Harry Rollins1. INSTITUTIONS (ALL): 1. Idaho National Laboratory, Idaho Falls, ID, United States.. PRESENTATION TYPE: Oral Preferred. ABSTRACT BODY: Abstract: Batteries with anodes consisting of alkali-containing materials (Li, Na, Mg & etc.) are practically feasible due to the formation of solid electrolyte interphase (SEI) films on the anode as a result of anode surface reactions with the electrolyte. The SEI governs the key performance metrics of the battery like calendar and cycle life, power, and safety. Conventional methods of SEI characterization are long, mostly ex-situ and do not provide metrics directly related to battery performance, which retards new battery development. The proposed presentation offers an overview of a new method and new precise metrics for in-situ SEI characterization and fast electrolyte selection for a specified alkali(-ion) battery. The new SEI electrochemical characterization metrics are in line with battery performance metrics. The method tracks the kinetics of SEI formation which contributes to fundamental science. From an applied science stand point the method may accelerate the development of new electrolytes for advanced batteries.. DECISION STATUS:. ABSTRACT STATUS: submitted Withdraw.

SUBMISSION ROLE: 2015 Northwest Regional Meeting. ABSTRACT SYMPOSIUM NAME: Interfaces and Electrochemistry for Energy Applications and Beyond - Oral - Invited. CONTROL ID: 2299823. TITLE: Electrochemical Upgrading for Production of Chemicals and Fuels. PRESENTER: Tedd Lister. PRESENTER (E-MAIL ONLY): tedd.lister@inl.gov. AUTHORS (FIRST NAME, LAST NAME): Tedd Lister1, Eric J. Dufek1, Lucia M. Petkovic2, Michael Lilga4, Asanga Padmaperuma3. INSTITUTIONS (ALL): 1. Idaho National Laboratory, Idaho Falls, ID, United States. 2. Mailstop 3632, Idaho National Laboratory, Idaho Falls, ID, United States. 3. Pacific Northwest National Laboratory, Richland, WA, United States. 4. Pacific Northwest National Laboratory, Richland, WA, United States.. PRESENTATION TYPE: Oral Preferred. ABSTRACT BODY: Abstract: Electrochemistry offers a novel method of upgrading low value materials to produce chemicals and fuels. Electrochemistry is poised to play a larger role in production as increased renewable electricity is introduced. Converting electrical energy directly to chemical bonds could answer future fuel and chemical challenges as petroleum becomes less accessible. Recent work at Idaho and Pacific Northwest National Laboratories has sought to translate electrochemical transformations from beaker to bench-scale. This presentation will discuss work in two areas: electrochemical reduction of CO2/H2O to H2/CO mixtures and electrochemical hydrogenation of biomass-derived oils.. DECISION STATUS:. ABSTRACT STATUS: submitted Withdraw.

SUBMISSION ROLE: 2015 Northwest Regional Meeting. ABSTRACT SYMPOSIUM NAME: Interfaces and Electrochemistry for Energy Applications and Beyond - Oral - Invited. CONTROL ID: 2299830. TITLE: ELECTROCHEMICAL PROCESS DEVELOPMENT FOR THE RECOVERY OF VALUE METALS IN END OF LIFE MOBILE ELECTRONIC DEVICES. PRESENTER: Luis Diaz Aldana. PRESENTER (E-MAIL ONLY): luis.diazaldana@inl.gov. AUTHORS (FIRST NAME, LAST NAME): Luis A. Diaz Aldana1, Tedd Lister1, Jacob A. Parkman1, Gemma Clark1. INSTITUTIONS (ALL): 1. Idaho National Laboratory, Idaho Falls, ID, United States.. PRESENTATION TYPE: Oral Only. ABSTRACT BODY: Abstract: Every year billions of mobile electronic devices (i.e. cellphones, tablets, and laptops) are sold around the world to replace aging technology. Although, many of these devices can go to a second life cycle after being refurbished, they eventually reach end of life. The combination of a growing market and a reduction in product lifetime urges the development of technologies for the recycling of end of life mobile electronic devices. These devices possess a significant amount of base and value metals, such as copper, nickel, palladium, gold, and silver, which can be found in concentrations that exceed those in mineral ores. An electrorecycling (ER) process concept has been developed for the selective extraction of metals using Fe3+ as the oxidant followed by recovery by electrowinning. In the electrowinning process the recovery of metals is coupled with the regeneration of the oxidizer (Fe3+), which provides a potential reduction, c.a. 50%, in the energy consumed by the currently employed electrowinning processes. In this work, development of the ER process will be presented for recovery of metals from mobile electronic devices.. DECISION STATUS:. ABSTRACT STATUS: submitted Withdraw.

SUBMISSION ROLE: 2015 Northwest Regional Meeting. ABSTRACT SYMPOSIUM NAME: Interfaces and Electrochemistry for Energy Applications and Beyond - Oral - Invited. CONTROL ID: 2299845. TITLE: The Electrochemical Nucleation and Physical Behavior of Hydrogen Nanobubbles. PRESENTER: Henry White. PRESENTER (E-MAIL ONLY): white@chem.utah.edu. AUTHORS (FIRST NAME, LAST NAME): Henry White1, Qianjin Chen1, Sean German1, Long Luo1. INSTITUTIONS (ALL): 1. University of Utah, Salt Lake City, UT, United States.. PRESENTATION TYPE: Oral Only. ABSTRACT BODY: Abstract: Gas nanobubbles formed at solid/liquid interfaces have received significant attention during the past decade due to their unexpected and remarkable stability. Interfacial nanobubbles may exist for hours or days, in contrast to their expected short lifetime (< 1 s) based on the theoretical rate of gas dissolution from a nanoscale bubble. Our laboratory has developed an electrochemical approach for investigating the formation and properties of a single nanobubble of H2 with a radius between 5 and 50 nm. To create an individual H2 nanobubble, a Pt nanodisk electrode, shrouded in a glass sheath, is used to reduce H+ in a concentrated acid solution, creating a supersaturated solution of H2 adjacent to the electrode surface. A liquid-to-gas phase transformation associated with the formation of a single nanobubble at the electrode surface is readily indicated in the voltammetric response by a sudden drop in H+ reduction current to near background levels. Due to their nanoscale dimensions, the Laplace pressure within these nanobubbles is on the order of ~100 atm. This address will describe measurements of the supersaturation of H2 required to electrochemically nucleate a H2 bubble, the critical size of the smallest stable H2 bubble nucleus, and the internal pressure within these nanobubbles. Electrochemical measurements of nanobubble also provide insight into the structure and chemical dynamics of electrochemical three-phase solid/liquid/gas boundaries, e.g., H+ reduction kinetics at a three-phase boundary, as well as estimation of the width of the three-phase boundary.. DECISION STATUS:. ABSTRACT STATUS: submitted Withdraw.