# The Recycling of Roadside Dust for Platinum Group Metals

Matthew P. Heaney

University of Nebraska at Omaha

# Author Note

The author of this manuscript is an undergraduate student at the University of Nebraska at Omaha.

Correspondence concerning this manuscript should be directed to Matthew P. Heaney

Email: mheaney@unomaha.edu

Abstract

The effects of human activity on the earth has presented numerous issues, many concerning the environment. Mining is one such issue that produces a noticeable negative effect on the environment. Human mining activity only increases as certain resources become progressively scarcer. Even early in human history precious metals were particularly sparse and required significant effort to collect a sizable amount. Even with industrial processes production is still rather slow due to low concentrations of metals and resources needed to extract metals. Recycling has been a popular way to increase efficiency of metal production such as aluminum, significantly reducing the resources used to repurpose it rather than extracting new rock. This same process should be replicable to precious metals, from the degradation of catalytic converters in cars and deposition of metals along the road.

The Recycling of Roadside Dust for Platinum Group Metals

Precious metal scarcity encourages development of newer more efficient methods of acquisition. With every method that is more efficient than the last a secondary effect occurs, the reduction of stresses on various systems. The systems put under this stress include, but are not limited to environmental, economic, and production. The result is typically positive overall for the systems, though some may be negatively impacted although for better. The stress reduced by the implementation of this research is not expected to be major given current production from mines. However, would be a benefit even currently and more so in the future as resources are expected to get progressively more depleted and need for them only increase. The implementation would certainly result in an increased palladium production given the relatively high concentrations of palladium found.

# Methods

Dust samples. Samples were collected in and around the city of Omaha, Nebraska each sample was collected either along the curb or the shoulder of the road. Initial samples contained various large debris from cars and discarded trash that had collected, such debris were removed by hand. Following debris removal samples were sieved through three progressively smaller openings, in the order 1cm, 300 micron, and 20 micron, yielding particulate <20 microns in size.

Chemicals. Fisher Scientific Certified ACS Plus grade nitric acid (70% concentration), Fisher Scientific Certified ACS Plus grade hydrochloric acid (36.5-38% concentration), Fisher Scientific (Crystalline/Certified), Palladium Chloride

Experimental. Standards were prepared for platinum and rhodium using diluted existing standards and had an according amount of nitric acid to have 2% concentration. Palladium standard was created using palladium chloride and 0.1 M hydrochloric acid. Three standards of each were created with concentrations of 100, 30, and 10 ppb, and a 2% nitric concentration.  Using concentrated nitric and hydrochloric acid mixed at a 1:4 ratio, respectively, to a total volume of 75 mL (15 mL nitric, 60 mL hydrochloric) of aqua regia. Aqua regia sample had 275mL of distilled water added, a 10.000 g dust sample was added, and immediately covered to prevent loss due to bubbling of decomposing carbonic acid. Upon the completion of decomposition for all carbonic acid <1 g. of potassium bisulfate was added to allow for the dissolution of rhodium into a complex. Solution was heated to just below boiling temperature and mixed using a heated magnetic stirrer and stir bar for 1 hour to allow for maximum dissolution of precious metals. Sample solutions were filtered twice using vacuum filtration to separate all insoluble compounds from solution. To separate clean 500 mL volumetric flasks, 77.50 mL of each sample solution was transferred via pipet and diluted to the mark resulting in a 2% nitric acid solution. Each sample was run through an ICP-MS with prepared standards to yield the results.

## Results1

ICP-MS analysis showed negligible concentrations of rhodium-103 and was unable to detect a reasonable amount. Platinum-195 concentrations were ranged from 0.3657 ppb at the I-680 and Blondo location to 0.1207 ppb at the N 124th St. location. Palladium-105 concentrations proved most abundant with 11.8598 ppb at the I-680 and Irvington, 8.4733 ppb at the I-680 and Blondo, and 3.4552 ppb at the N 124th St. locations. Concentrations were then calculated for other isotopic abundances and measured in total to grams per metric ton. Platinum concentrations ranged from 0.08 g/metric ton to 0.25 g/metric ton, and palladium concentrations ranged from 3.52 g/metric ton to 12.08 g/metric ton.

### Tables.

ICP-MS Platinum and Palladium Concentrations.

| Sample Location | Pd105 ppb | Pt195 ppb |
| --- | --- | --- |
| Blondo and I680 | 8.4733 | 0.3657 |
| Irvington and I680 | 11.8598 | 0.1977 |
| N 124th St. | 3.4552 | 0.1207 |

Isotopic Abundances.

| Palladium Isotope; Percent Abundance. Pd-102; 1.020%. Pd-104; 11.140%. Pd-105; 22.330%. Pd-106; 27.330%. Pd-108; 26.460%. Pd-110; 11.720%. | Platinum Isotope; Percent Abundance. Pt-192; 0.78%. Pt-194; 32.86%. Pt-195; 33.78%. Pt-196; 25.21%. Pt-198; 7.36%. |
| --- | --- |

Final Calculated Concentrations.

| Sample Location | Pd (g/metric ton) | Ag (g/metric ton) | Pt (g/metric ton) |
| --- | --- | --- | --- |
| Blondo and I-680 | 8.6302575 | 11.79324 | 0.246327 |
| Irvington and I-680 | 12.0777075 | 137.4831075 | 0.1335975 |
| N 124th St. | 3.518655 | 0.70641 | 0.0814275 |

##### Discussion.

Comparing these results to the concentrations found in mines can be difficult as often mines provide values for all platinum group metals found in a tonne of ore, and not each individual metal. Though grading systems have been adopted to determine the quality of metal content, however they are often dependent on which mine is being referenced. However, the consensus is that “one would look for grades of 6 grams platinum + palladium/ tonne… as a reasonable thresh-old for high-grade” (Stewart, 2017). Though in the case of specific mines where concentrations are high, they may measure by the mill-head grade, which is an average concentration in ore. One such mine was the Stillwater Mine in Nye, Montana stating “The mill-head grade was 16.8 grams per metric ton (g/t) of combined palladium and platinum, compared with 19.6 g/t in 2001” (Hilliard, 2003). Few, if any, mines have a concentration of this magnitude, however this is for both the platinum and palladium content and since the results showed notable levels of palladium, the palladium content may be even higher than that of Stillwater Mine. Therefore the recycling of roadside dust could prove to be far more effective method of precious metal collection and production than most mines, with far less of an environmental impact.

# References

- Rosman, K.J.R., Taylor, P.D.P. (1999). Pure Appl. Chem, 71, pp. 1593-1607.

- Hilliard, H. E. (2003). Platinum Group Metals. U.S. Geological Survey Minerals Yearbook, pp. 58

- Stewart, A. (2017). Making the Grade: Understanding Exploration Results. Resource World.

Acknowledgement

I am grateful to all the faculty of the University of Nebraska, Omaha who helped provide me with the necessary support, materials, and equipment to perform my research. The two most notable faculty being, Dr. Dana Richter-Egger, Ph.D. and Dr. Edmund Tisko, Ph.D. As well as Cody Don Reeder from Utah State University for giving me the inspiration to perform this research.

K.J.R. Rosman, P.D.P. Taylor Pure Appl. Chem. 1999, 71, 1593-1607.